## Slide 1: SARNET Source Term Comments on the Draft ISTC Proposal VERONIKA Edited by T. Haste (PSI), P. Giordano (IRSN) and L.E. Herranz (CIEMAT) from the contributions of: Z. Hozer (AEKI), G. Ducros (CEA), Y. Dutheillet (EDF), N. Davidovich (ENEA) R. Dubourg (IRSN), D. Bottomely (JRC/ITU) and S. Güntay (PSI)
CEG-SAM-10 meeting
Kurchatov-City, Republic of Kazakhstan, IAE NNC, Sept. 5-8, 2006

## Slide 2: OUTLINE
Overview of the VERONIKA Project Proposal
Procedure & Schedule
Specific Comments
Generic Remarks
Final Test Matrix

## Slide 3: Overview of the VERONIKA Project Proposal
PART A. VVER Fuel-FPR: To obtain experimental data on FPR from highly irradiated VVER fuel and fuel micro-structure evolution
PART B. MFPR: To develop and validate the MFPR models based on data from PART A.

## Slide 4: Procedure & Schedule
CEG-SAM submission for review by the ST area (April 7th, 2006)
Distribution to WP14-1 partners
Collection of replies
Discussion between ST Coordinator and Sub-manager of the proposal
Issue of a technical note with SARNET-ST comments (May 31st, 2006)

## Slide 5: Specific Comments (1/3)
Address the whole range of oxygen potential: H2/H2-H2Ov/H2Ov/air
Measurement of the oxidation state of the clad before the test
Define the experimental technique to be used to de-clad fuel
Need for fuel characterization (i.e., grain size, natural and/or artificial damage, etc.)
Define TH conditions (i.e., gas flows, composition of mixtures) more accurately
Care about re-irradiation history and crucible material!
Enable MFPR (if needed) to deal with highly oxidizing conditions
Boundary Conditions
 Recommendations
 Valuable ST information
Plant calculations to identify relevant fuel and coolant conditions of air-ingress scenarios
PHEBUS-FP experience

## Slide 6: Specific Comments (2/3)
Similarity to VERCORS and VERDON programmes
Comparisons to VERCORS could provide insights on the fuel effect (W-PWR vs VVER)
Future tests definition should take into account results as they appear
Relationship with other projects
 Observations
Post-test examinations: use of EPMA/SEM, SIMS and TEM
On-line measurements: counting rate adjust by using different collimator slits?
Conduct a null test to characterize local boundary conditions round the crucible
Detailed experimental matters
 Recommendations

## Slide 7: Specific Comments (3/3)
Use B4C and steel next to the fuel sample (release enhancement by eutectic formation!)
Extension to the scope
 Recommendation

## Slide 8: Generic Remarks
Technical support to the proposal from SARNET-ST
Appreciation for the systematic nature of the test matrix

## Slide 9: Last Test Matrix Proposed
 Observations
No steam tests in this new proposal!
He substituted for Ar
Experimental techniques to be used not stated