## Slide 1
INVESTIGATION OF FISSION PRODUCT RELEASE FROM HIGH BURN-UP FUEL ANNEALED UNDER OXIDIZING AND REDUCTION CONDITION
9th CEG-SAM Meeting
March 7-9, 2006
Paris
VERONIKA
(VVER Experiments on Release due to Over-heating: Normalization and Knowledge Augmentation).
Project Proposal
RIAR (Dimitrovgrad), IBRAE (Moscow)
International Science and Technology Center

## Slide 2: Objectives of VERONIKA Project
To obtain detailed experimental data on fission products behaviour and release from highly irradiated VVER fuel along with fuel micro-structure evolution under severe accident conditions
To use these results for the development (and validation) of the physical models and numerical codes describing fuel behaviour and fission products release

## Slide 3: Tasks of VERONIKA Project
To obtain new detailed experimental data on fuel microstructure, FP release and behaviour under the insufficiently investigated conditions for PWR and VVER high burn-up fuel
Basing on results of the new experiments, to obtain data missing for FP release modelling and code development
To improve existing physical models, to develop and validate the codes predicting FP release under severe accident conditions basing on the existing and newly obtained data for VVER fuel
To compare FP release from high burnup VVER and PWR fuel, to reveal the effects connected with peculiarity in manufacturing techniques and in operational characteristics

## Slide 4: Parts of VERONIKA Project
Part A: VVER FUEL-FPR
Experimental study of fuel behaviour and fission products release at temperatures and gas environments typical for severe accidents
Part B: MFPR
Improvement of models and codes for description of fission products and highly irradiated VVER fuel behaviour under conditions of severe accidents without fuel melting

## Slide 5: International Collaboration in VERONIKA Project
High cost and man-power of experimental researches in the field of nuclear safety lead to necessity of a wide international co-operation
Such collaboration is currently developed and coordinated in the framework of the European SARNET program (6th Framework Programme of EC)
VERONICA is seen as complementary Programme to the previous (VERCORS) and future (e.g. VERDON) European Projects
Experience of collaboration of Russian participants with European partners within 4th FP (CIT, COBE), 5th FP (COLOSS) and ISTC Projects (e.g. ##1648.2, 2936) is favourable for success of the new Project

## Slide 6: FP release tests carried out at RIAR (1)
Despite RIAR experiments were performed under more simple conditions in comparison with severe accidents:
  oxidizing gaseous atmosphere were used only at temperature <1200°С, no tests in reducing atmosphere, etc.,
the obtained experience and technical approach will be realized for manufacturing of a new experimental rig and performance of new tests in the proposed Project

## Slide 7
Burn-up - 41,7 MW*d/kg U
Temperature - 1200°С
Caesium release – 85%.
Krypton release - 74%
Fuel oxidation –UO2,21
FP release tests carried out at RIAR (2) Fuel specimen oxidation in steam-argon flow

## Slide 8: Scope of VERONIKA Project Tests
Investigation of fission products release from fuel with burnup of 60 MW*d/kgU in steam, steam-hydrogen and hydrogen environments in the temperature range of 1400 - 2300oC typical for severe accidents at NPP
Investigation of the release of a wide list of fission products including short living isotopes: 85Kr, 133Xe, 131I, 137Cs, 134Cs, 106Ru, 103Ru, 144Ce, 99Mo, 140Ba, 95Zr and other. That will be provided by pre-irradiation of the specimens in the research reactor MIR
Accurate representation of evolution of high burn-up fuel microstructure under tests conditions (by pre- and post-test microanalysis of samples)
Determination of hydrogen generation and extend of fuel oxidation.

## Slide 9: Project Stages
Project total duration (2 stages) - 5,5 years
All work is planned to be carried out in two stages to provide the important feedback necessary for long-term projects. This will allow:
  correction of the test matrix in the second stage, if needed, depending on the results of the first stage
  interaction with other projects in progress
First stage (3 years):
4 experiments in pure steam at 1400 and 2300°С
6 experiments in inert-reducing atmosphere at 1400, 1700 and 2300°С
Second stage (2.5 years):
10 tests in steam-hydrogen mixtures at 1400, 1700 and 2300°С
test series will be specified by the results of the first stage

## Slide 10
Gas environment |  | Test temperature,°C |  | 
 |  | 1400 | 1700 | 2300
H2O | 25 | T1, T2 | - | T1, T2
(H2O/H2)1 | 25/0,45 | T1, T2 | T1, T2 | T1, T2
(H2O/H2)2 | 25/0,2 | T1, T2 | - | T1, T2
H2/He | 0,45/5 | T1, T2 | T1, T2 | T1, T2
Test Matrix
Altogether 20 tests (during 2 stages of Project): 10 tests with segments of fuel rods (T1) and 10 tests with fuel pellets (T2)
Test matrix is aimed at 3 goals: 1. To determine the influence of gas medium (H2O, (H2O/H2)1, (H2O/H2)2, H2/He) on FP release from specimens with and without cladding 2. To determine the influence of temperature (1400, 1700 and 2300 °С) on FP release from specimens with and without cladding at the same gas-steam mixture content 3. To determine the influence of fuel-cladding interaction in the reducing gas medium on FP release at temperatures of 1400, 1700 and 2300 °С
Flow rate,
mg/s

## Slide 11
Test Matrix (1st stage)
# Test | Sample type | Environ-ment | Test temperature,°С | Post-test examination |  | 
 |  |  |  | Metallo-graphy | EPMA, SEM | Oxygen factor
1 | Fuel rod segment | Н2 /Не | 1400 | + | + | -
2 | Fuel rod segment | Н2 /Не | 1700 | + | + | -
3 | Fuel rod segment | Н2 /Не | 2300 | + | + | -
4 | Bare fuel | Н2 /Не | 1400 | + | + | -
5 | Bare fuel | Н2 /Не | 1700 | + | + | -
6 | Bare fuel | Н2 /Не | 2300 | + | + | -
7 | Fuel rod segment | Н2 О | 1400 | + | - | +
8 | Fuel rod segment | Н2 О | 2300 | + | - | +
9 | Bare fuel | Н2 О | 1400 | + | - | +
10 | Bare fuel | Н2 О | 2300 | + | - | +
11 | Reference sample of initial irradiated fuel |  |  | + | + | -

## Slide 12: Main Test Procedures
Manufacturing of the experimental rig
Preparation and certification of fuel specimens (fuel pellets and fragments of fuel rods)
Pre-irradiation in the reactor MIR
Performance of FP release tests
Post-test examination of fuel specimens

## Slide 13: Test Rig
Steam overheater
(800°С)
Heater(150°С)
Condenser
Filter-
dehydrator
Water collector
Additional filter
Flow meter
Ceramic tubes
(ZrO2, Al2O3, Al2O3)
HF coil
Pyrometer
Inlet gas line
Main channel
(ZrO2)
Main filter
Carrier gas line
(in the case
of pure steam
environment)
Gamma-spectrometer
(FP measurement
in the filter)
Gamma-spectrometer
(FP measurement
in the specimen)
Protective gas line
Specimen
holder
Specimen
Pressure
transducer
Hot cell
Gamma-spectrometer
(GFP measurement)
Intel steam line
H2
He
Mass spectrometer

## Slide 14: Test Samples
2 kinds of samples
  Segments of the fuel rod (pellet in the genuine cladding without end cups)
  Fuel pellet without cladding (fragments of fuel pellet)
Procedure of sample preparation
  Certification of irradiated VVER fuel rod
  Manufacturing of refabricated fuel rods
  Short irradiation of the refabricated fuel rods in the research reactor for accumulation of short-lived fission products (at low power and low temperature)
  Certification of the irradiated refabricated fuel rod
  Preparation of samples from the irradiated refabricated fuel rod

## Slide 15: Test Performance
Test temperature
  heating in the inert atmosphere up to the temperature of 600 °C
  heating from 600 up to 1400 °C with a rate of 5 K/s
  annealing at 1400 °C during 1 hour
  heating with a rate of ~ 1 K/s up to the specified temperature (1700 or 2300 °C)
  annealing at the attained temperature within 30 minutes
  end of heating
Parameters to be measured during the test
  intensity of GFP in the running gas coil
  intensity of FP in a fuel specimen
  intensity of FP on the main filter
  hydrogen concentration in the carrier-gas after passing through the heater
Results to be obtained
  relative FP release
  hydrogen generation

## Slide 16: Post-Test Examinations
Optical metallography
  grain size
  porosity
  gas swelling
EPMA and SEM analysis
  local content and radial distribution of fission products
  elemental content of precipitates in the fuel
Determination of fuel stoichiometry

## Slide 17: Part B. MFPR (Model for Fission Products Release)
Objectives
  On the base of new experimental results:
  to develop theoretical models of fission products and irradiated VVER fuel behaviour under conditions of severe accidents
  to improve and to adapt physical models and codes developed for PWR fuel to VVER fuel

## Slide 18: MFPR Code Features
Development
  IBRAE-IRSN co-operation (1995-2006)
Mechanistic description
of FP behavior in irradiated UO2 with intact geometry
  in irradiation regime : steady state and transients
  in annealing regime : steady state and transients
  in accidental conditions: LOCA, severe accidents
Two kinds of mechanistic models
  Fission gases and gas bubbles
  Chemically active elements
   And also…
    Interaction between the two models
    Fuel oxidation/vaporisation in steam/hydrogen/inert mixtures
    Evolution of fuel microscopic defect structure

## Slide 19: MFPR Basic Models
Intragranular gas atoms
-
diffusion towards grain boundary (
С
concentration)
-
bubble nucleation & capture by bubbles
-
capture by dislocations
-
directio
nal diffusion by
С
T
-
grain
-
boundary sweeping, dislocation creep
Intragranular bubbles
-
nucleation and coalescence
-
capture of gas atoms
-
loss of gas atoms by re
-
solution (thermal & recoil)
-
di
ffusion towards grain boundaries (face bubbles):
directional diffusion by
С
T, grain
-
boundary sweeping,
dislocation creep, vacancy gradient.
-
Face bubbles
-
fed by gas atoms, intragranular bubbles
& vaporizati
on of condensed
-
phase species
-
growth & interconnection leading to release
into edge bubbles
Intergranular
zone
Edge bubbles
-
supplied by face bubbles
-
swelling until a critical threshold
-
release into open porosities
Intragranular
zone
Precipitates
-
fed by intragranular diffusion of non
-
gas FPs
-
formation of 3 condensed phases at grain boundary:
ternary (e.g.
Cs
2
MoO
4
),
CsI
& metallic (
Ru
,
Mo, Sb
)
-
equilibrium between precipitates, face bubbles,
UO
2+x
Dislo
cations
-
creep towards grain boundaries
-
trapping of intragranular gases
(atoms & bubbles)
Grain
-
growth & boundary sweeping

## Slide 20: Transport of Fission Gases
Diffusion of gas atoms (Cg)
Intragranular bubbles (Cb, Nb) nucleation, growth and resolution (thermal and irradiation-induced)
Intragranular bubbles diffusion (also biased in temperature gradient) and coalescence
Interactions with dislocations (d), sintering pores (Cp), vacancies (Cv) and interstitials (Ci)
Intergranular bubbles formation, coalescence and interconnection...
X = {Cg, Cb, Vb, d, Cd, Vp, Cp, Cv, Ci}
System of equations:

## Slide 21: Transport of Chemically Active FP
CHEMICALLY ACTIVE ELEMENTS
Cs, Ce, I, Eu, Mo, Nd, Ru, Nb, Ba, Sb, Sr, Te, Zr, Xe, La
Grain Boundary (GB)
Boundary conditions:
thermo-chemical equilibrium between various phases on GB
Release: subsequent migration of FP elements in the form of gaseous compounds to open porosity
Transport equation in solid solution:
SOLID SOLUTION
Gas phase
Grey
CsI
Metal
Diffusion
PRINCIPAL PHASES
Fuel-FP oxide solid solution:
Cs(c);
Ba(c), Sr(c) and BaO(c), SrO(c);
Zr(c), ZrO2(c), Nb(c), NbO(c), NbO2(c);
La(c), Ce(c), Eu(c), Nd(c), and their oxides LaO3/2(c), CeO3/2(c), CeO2(c), EuO3/2(c), EuO(c), NdO3/2(c);
Sb(s) and SbO3/2(c);
Mo(s), Ru(s) and MoO2(c), RuO2(c).
Metal phase: Mo(c) and Ru(c).
Grey phase (complex ternary compounds):
BaUO4(c), SrUO4(c), Cs2UO4(c),
BaMoO4(c), SrMoO4(c), Cs2MoO4(c),
BaZrO3(c), SrZrO3(c), Cs2ZrO3(c).
Separate solid phase: CsI(c).
Gas phase: Xe(g), Te(g), I(g), Cs(g), CsI(g), Cs2MoO4(g), MoO3(g), (MoO3)2(g), (MoO3)3(g), RuO(g), RuO2(g), RuO3(g), Ba(g), Sr(g), ZrO(g), LaO(g), CeO(g), NdO(g), NbO(g), O2(g).

## Slide 22: MFPR Validation
Scope
  Steady irradiation
  Transient
  Post-irradiation annealing
Results
  Microstructure (evolution of intra- and intergranular bubbles)
  FP release (gas, volatiles, semi- and non-volatiles)
  Fuel swelling (total, intra- and intergranular)
Qualification and validation against
  Separate-effect tests with fuel samples
  Semi-analytical out-of-pile tests: VI (USA), UCE (Canada), VERCORS (France), RIAR, etc.
  Large scale in-pile tests: HALDEN, PHEBUS FP

## Slide 23
Release kinetics of Mo
Release kinetics of Ba
Simulation of semi-analytical out-of-pile tests
VERCORS-4 (CEA)
Examples of MFPR Validation

## Slide 24
MFPR Tasks in VERONIKA Project
Pre-test calculations of new experiments for determination of parameters and conditions of the tests
Processing and analysis of results of new experiments
Development and improvement of the physical models on fission products release and high burnup VVER fuel behaviour under conditions of severe accident
Implementation of the developed and improved models in the MFPR code
Verification of the MFPR code against the new experimental database and other new available data at the end or during the program

## Slide 25: Project Costs
The first stage
(3 years duration, 777 400 $) :
Т10 – beginning of the work under the project;
Т10+1 year – manufacturing and testing of the experimental rig, 315 k$;
Т10+1 year - adaptation of the MFPR code to the new experimental rig, pre-test calculations, 26.2 k$;
Т10+2,5 years – first series of tests (10 tests), 346.2 k$;
Т10+3,0 years – theoretical analysis of the obtained experimental data, development of models and codes, 80 k$.
The second stage
(2.5 years duration, 494 000 $):
  Т20 – beginning of the second stage work;
  Т20+1 year – second series of tests (10 tests), 343 k$;
  Т20+2.5 years –post-test specimen examinations; theoretical analysis of the obtained experimental data, development of models and codes, 151 k$.
The estimated total cost of the Project (2 stages) – 1 217 400 $