## Slide 1
Progress Report on the ISTC Project # 3876
Thermal Hydraulics of U-Zr-O molten pool under oxidising conditions in multi-scale approach (crucible - bundle - reactor scales)
Short title: THOMAS
(Thermal Hydraulics of Oxidising Melt in Severe () Accidents)
Presented by
M.S. Veshchunov (IBRAE)
18th Meeting CEG-CM
St. Petersburg, Russian Federation
Hotel “Ambassador”
September 28-30, 2010
International Science and Technology Center

## Slide 2
General Information
Leading Institution: | IBRAE, Moscow
Duration: Commencement: | 3 years October 2008

## Slide 3
Non-CIS Collaborators
FZK | Forschungszentrum Karlsruhe GmbH | Germany Karlsruhe
ITU | European Commission Joint Research Centre Institut für Transurane | Germany Karlsruhe
IRSN | Institut de Radioprotection et de Sûreté Nucléaire | France Cadarache
CEA | Commisariat à l’Energie Atomique | France Cadarache
IVS Trnava | Inžinierska výpočtová spoločnosť Trnava, s.r.o., | Slovak Republic

## Slide 4
Project Objectives
On the base of analysis of available test data from small - and large - scale experiments, to develop a mechanistic description of U-Zr-O molten pool behaviour in oxidising conditions.
For this purpose, to carry out a tight coupling of the two advanced numerical tools developed within the previous ISTC Project #2936: the SVECHA physico-chemical (molten pool oxidation) model and the 3D thermo-hydraulic code CONV.
This will allow extension of thermal hydraulic consideration of oxidised melt from small scales (crucible tests) up to a large scale (reactor pressure vessel), including an intermediate scale corresponding to molten pools in bundle tests.
As a result, improved interpretation of the Phebus FP bundle tests observations of corium melt oxidation, as well as transposition of thermal hydraulic consideration from test to reactor scale, are foreseen.
The developed and verified models will be further used for benchmarking and improvement of simplified models of various system codes such as ICARE/CATHARE, ASTEC or Russian severe accident code SOCRAT.

## Slide 5: Technical Schedule
Task 1. Development and Improvement of the Physico-Chemical Model for the U-Zr-O Melt Oxidation on the Base of New Crucible Tests (1-6 QUATERS)
Task 2. Development and Improvement of the Unified Thermal Hydraulic Technique (CONV Code) for Simulation of Multiphase Processes in Complex Domains of Convectively Stirred Melt (1-6 QUATERS)
Task 3. Tight Coupling of the Two Advanced Tools: the Physico-Chemical (Molten Pool Oxidation) Model and the Thermo-Hydraulic Code CONV, for Realistic Mechanistic Description of U-Zr-O Molten Pool Behaviour in Oxidising Test Conditions (7-10 QUATERS)
Task 4. Extension of the Thermal Hydraulic Consideration of Oxidised Melt from Small Scale (Crucible Tests) up to a Large Scale (Reactor Pressure Vessel), Including an Intermediate Scale Corresponding to Molten Pools in the Bundle Tests (11-12 QUATERS)

## Slide 6
Calculates:
U-Zr-O melt composition and average temperature
U-Zr-O melt oxidation and bulk ceramic precipitates formation
UO2 pellet dissolution
(Zr,U)O2 peripheral crust thickness and temperature distribution
Melt blockage relocation
Validated against:
FZK crucible tests
CORA (melt relocation)
Phebus FPT 0&1 (molten pool oxidation)
2-d Model for Molten Pool Oxidation and Relocation (previous ISTC Project #2936)

## Slide 7: 2-d Molten Pool Oxidation Model (Mass Transfer)
x1
x2
x3
x4
r2
r3
U-Zr-O melt
(Zr,U)O2 oxide
r1
r4
FeO
VS
Mass flux matches
Mass balances
Additional layers
Additional equations

## Slide 8
Heat flux matches
Heat balance
2-d Molten Pool Oxidation Model
(Heat Transfer)
melt
boundary layer
Oxide crust
VS
FeO
Rmp
T
Tmp
Tint
Tox
Ts
Tout
r
Lox
LFeO

## Slide 9: METCOR observations
Drop in the oxygen potential of the melt is detected when heated steel has a high oxidation rate
Lower corrosion rate at the final stage of experiment is explained by the insufficient air supply to the melt and by its decreased oxygen potential
Conclusion:
Corrosion rate notably depends on the oxygen potential of the melt
Therefore, a theoretical model has to take into consideration oxygen transport through the interaction layers, which should be self-consistently calculated with Fe ions diffusion (through FeO layer)

## Slide 10
Oxygen diffusion through solid crust (UO2+ZrO2 melt)
Solution of diffusion equation 
Zr-O phase diagram considered as pseudo-binary for U-Zr-O
U-Zr-O melt
T
cmin(T+)
cO
(U,Zr)O2
x
SS
Jox
T+
T-
cmin(T-)
FeO
t = 0

## Slide 11: SS oxidation model
SVECHA model
Parabolic correlation from METCOR tests (15 Kh2NMFA vessel steel)
“Oxygen starvation” regime: oxygen flux Jox through the crust (above calculated) is rate controlling during relatively long period of interactions
T=1273 K

## Slide 12: METCOR observations
Conclusions:
In “low temperature” tests corrosion thickness ( 1 mm) roughly coincides with FeO thickness (i.e. steel is “substituted” by oxide), whereas in “high temperature” tests FeO ( 5 mm !!) is completely “extruded” through the crust
A theoretical model has to take into consideration the “drainage” mechanism
Interaction zone in MC-2 test
Low temperature tests
High temperature tests
Initial position of specimen surface
FeO corrosion layer
Steel
Interaction zone in MCP-2 test
Steel
Crust
Initial position of specimen surface
5 mm

## Slide 13: Observations in earlier tests
A similar effect of rapid eutectic penetration in vessel steel interacting with hot ceramic material (fuel or crust) was described in the literature (in 80-90-ies): “The normal melting point of the steel is around 1700 K, but chemical interactions between fuel and the steel components are likely to lower the effective melting temperature of the steel. The rapid eutectic penetration temperature is approximately 1400 K. Melt-through of the reactor vessel might occur if direct contact with fuel was established and the vessel cooling was insufficient to maintain the local wall temperature below the effective melting temperature” [SA research Review paper for Fast Breeder Reactors, Report ANL-2010]
A similar effect of steel corrosion acceleration and melt-through, owing to steel liquefaction on the interface between the steel wrapper and U-Zr-O corium crust and “drainage” of the formed melt into corium, was observed in the French tests SCARABEE
METCOR tests provide some additional (above presented) microstructure observations that allow qualitative clarification of the “drainage” mechanism (of eutectic melt) earlier observed in the integral tests (despite such mechanism was rejected by the METCOR team !)

## Slide 14: Physical mechanisms of enhanced SS corrosion at high temperatures
“Flowering” mechanism:
  formation of FeO/crust eutectic melt and its extrusion (or “drainage”) through the crust
Low temperatures
High temperatures
Melt
Crust
FeO
Initial position of Fe boundary
Compressive stresses
Tensile stresses
Cracks and tears
Melt
Crust
FeO
Eutectics
Melt
SS
SS

## Slide 15: Development of the 1-D numerical module for U-Zr-O corium melt - steel oxidation
Transformation of the 2-D stand-alone numerical model (for the simplified geometry of the tests) into the 1-D corium melt - steel oxidation model, in order to describe local interactions at the corium-steel interface (in the geometry of the pressure vessel)
This allows to exclude a simplified description of the heat and mass exchange between the U-Zr-O corium melt and crust, and to use (in future) detailed thermo-hydraulic approach of the CONV code
Development of the interface between the 1-D module (melt–steel oxidation) and the 2-D thermo-hydraulic code (U-Zr-O corium melt), in order to implement the module into the code

## Slide 16: 1D model for U-Zr-O corium melt - steel oxidation
U-Zr-O corium melt temperature and composition evolutions are calculated in 2-D thermo-hydraulic code
Oxidation module calculates the solid phases thicknesses, temperatures and U, Zr, O fluxes into melt
Oxidation module is coupled with 2-D thermo-hydraulic code through the heat flux and oxygen mass flux at the melt-solid interface

## Slide 17: Simulation of crust growth and SS corrosion by 1-d model
Temperature evolution under fixed boundary conditions:
2. Unlimited oxygen supply to the corrosion layer (through the crust)
1. Oxygen supply to the corrosion layer limited by diffusion transport through the crust (“starvation effect”)

## Slide 18: Simulation of crust growth and SS corrosion by 1-d model
Crust, corrosion and oxide layers evolution:
2. Unlimited oxygen supply to the corrosion layer (through the crust)
1. Oxygen supply to the corrosion layer limited by diffusion transport through the crust (“starvation effect”)

## Slide 19
Recalculation of U, Zr, O concentrations, temperature, heat flux and oxygen mass flux in the melt at the melt-solid boundary from 2-D CFD code results
Calling of 1-D oxidation module in each thermo-hydraulic spatial mesh at the melt-solid boundary at each time step produced by 2-D CFD code
Recalculation of 1-D oxidation module results for solid phases thicknesses, temperatures and U, Zr, O fluxes into boundary conditions for 2-D CFD code
Melt 2D Temperature,
Concentrations, Velocity
at t(n+1) = t(n) + Δt
Boundary melt Temperature,
U, Zr, O Concentrations,
Oxygen Flux, Heat flux
1-D oxidation Module
Solid phase boundary Position,
Temperature,
Mass sources
at t(n+1) = t(n) + Δt
Interface program for 1-D oxidation module coupling with the corium melt 2-D CFD code

## Slide 20: Conclusions
The 2-D stand-alone code developed to simulate (in the simplified geometry of the tests) simultaneous UO2 fuel dissolution, U-Zr-O corium melt oxidation accompanied with the bulk ceramic precipitates formation and oxidation of the steel wall of a vessel in contact with corium, was transformed in the previous stage of the Project (Quarters 5-6) into the 1-D corium melt-steel oxidation module, in order to describe local interactions at the corium-steel interface (in the geometry of the pressure vessel). This allowed to exclude from the code a simplified description of the heat and mass exchange between the U-Zr-O corium melt and peripheral crusts, and to use (in future) detailed thermo-hydraulic approach of the CONV code.
The work on further development and testing of the 1-D oxidation numerical module that simulates evolution of the solid phase layers ((Zr,U)O2-x crust, FeO corrosion layer and steel), temperature distributions in the layers and U, Zr, O molar fluxes into the melt, was continued.
The interface program unit for coupling of the melt-steel oxidation 1-D module with the corium melt 2-D thermo-hydraulic code is under development.