## Slide 1
1
Progress Report on the ISTC Project # 3876
Thermal Hydraulics of U-Zr-O molten pool under oxidising conditions in multi-scale approach (crucible - bundle - reactor scales)
Short title: THOMAS
(Thermal Hydraulics of Oxidising Melt in Severe () Accidents)
Presented by
M.S. Veshchunov (IBRAE)
19th Meeting CEG-CM
Pisa, Italia
March 14-16, 2011
International Science and Technology Center
Notes: f;jhg;\jd
1

## Slide 2
General Information
Leading Institution: | IBRAE, Moscow
Duration: Commencement: | 3 years October 2008

## Slide 3
Non-CIS Collaborators
FZK | Forschungszentrum Karlsruhe GmbH | Germany Karlsruhe
ITU | European Commission Joint Research Centre Institut für Transurane | Germany Karlsruhe
IRSN | Institut de Radioprotection et de Sûreté Nucléaire | France Cadarache
CEA | Commisariat à l’Energie Atomique | France Cadarache
IVS Trnava | Inžinierska výpočtová spoločnosť Trnava, s.r.o., | Slovak Republic

## Slide 4: Tasks of the Work Plan
4
Task 3. Tight Coupling of the Two Advanced Tools: the Physico-Chemical (Molten Pool Oxidation) Model and the Thermo-Hydraulic Code CONV, for Realistic Mechanistic Description of U-Zr-O Molten Pool Behaviour in Oxidising Test Conditions (7-10 QUATERS)
Subtask 3.3. Implementation of physicochemical melt oxidation model for modeling of thermal hydraulic behavior of U-Zr-O melt under oxidizing for small and medium scale experiments in code CONV 2D.
State / Situation at the beginning of the current quarter
The melt oxidation model was modified and upgraded to the geometry of molten pool confined by the walls of reactor pressure vessel (i.e. 1D version was developed for coupling with CONV 2D in each radial mesh).
Preparatory work with the CONV 2D code sources for implementation of melt oxidation model was finished.
Notes: f;jhg;\jd
4

## Slide 5: U-Zr-O Corium Melt - Steel Oxidation 1D model
U-Zr-O corium melt temperature and composition evolutions are calculated in 2-D thermo-hydraulic code
Oxidation module calculates the solid phases thicknesses, temperatures and U, Zr, O fluxes into melt
Oxidation module is to be coupled with 2-D thermo-hydraulic code through the heat flux and oxygen mass flux at the melt-solid interface

## Slide 6: Modification of the Basic Computation Cycle of CONV2D
6
The basic computation cycle of CONV2D was modified and supplemented with a call to the melt-steel oxidation 1-D module.
Initialization of the initial and boundary conditions CONV2D
Bases calculation cycle
Heat conductivity block (convection + diffusion)
Hydrodynamics block (calculation of the velocities and pressure)
Output of the results (2d-temperature fields, heat fluxes, 1d characteristics of the task)
Transformation of data to format of the
melt-steel oxidation
1-D module
Melt-steel oxidation 1-D module
Transformation of data to CONV2D format
Notes: f;jhg;\jd
6

## Slide 7: Interface and Input-Output Parameters
7
The interface between the melt-steel oxidation 1-D module and the corium melt 2-D thermal-hydraulic code was elaborated:
  List of necessary parameters for joint work of two modules was specified;
  Interchanging of variables were reduced to uniform standard form (i.e. lack of the common blocks and interior allocation of memory).
Input-Output parameters of the melt-steel oxidation 1-D module
Input | Output
RINTS - vessel wall internal radius ROUTS - vessel wall outer radius GSTEP - time step FSFLW - heat source due to fission heat, homogeneously generated in the melt and in the solid crusts TMELT - melt temperature at the boundary with the solid crust TOUTS - outer surface temperature of the vessel wall UZROHF - heat flux from the melt UZROMF - Oxygen mass flux from the melt | FPRES - volume fraction of solid precipitates CO - oxygen distribution in oxide crust RSOLID(1) - radius at internal surface of oxide RSOLID(2) - radius at boundary of oxide crust with steel oxide RSOLID(3) - radius at steel internal surface TSOLID(1) - temperature at internal surface of oxide TSOLID(2) - temperature at boundary of oxide crust with steel oxide TSOLID(3) - temperature at steel internal surface DYODT - oxygen flux in to the melt
Notes: f;jhg;\jd
7

## Slide 8: Coordination of Grids
8
Adaptation CONV2D in a part of the coordination of the grid data with melt-steel oxidation 1-D module is carried out:
An auxiliary calculation grid r-φ is generated;
The subprograms for data transformation from a rectangular grid to r-φ grid and back are developed.
Rectangular grid
r-φ grid
Notes: f;jhg;\jd
8

## Slide 9: Data Exchange between the Modules
9
Data transferred from CONV2D to the melt-steel oxidation 1-D module (e.g. value of temperature at the crust boundary, heat flux, etc.) are transformed from the rectangular to the auxiliary r-φ grid. In response CONV2D receives from 1-d module data for crust coordinates and oxygen flux, which are transformed back to the rectangular grid of CONV2D.
Steel Vessel
Crust
Rasplav
Heat Flux,
Melt Temperature
R solid,
Oxygen Flux
Notes: f;jhg;\jd
9

## Slide 10: Conclusions
10
Implementation of the melt-steel oxidation 1-d module in the CONV2D code for modeling of thermal hydraulic behavior of U-Zr-O melt under oxidizing conditions, was carried out.
The basic computation cycle of CONV2D was modified and supplemented with a call to the melt-steel oxidation 1-D module.
The interfaces of the two modules were coordinated:
  List of necessary input-output parameters for joint operation of the two modules was specified; the interchanging of variables were reduced to uniform standard form (i.e. lack of the common blocks and interior allocation of memory) ;
  Auxiliary calculation grid r - φ was generated; the subprogram for data transformation from rectangular grid to r - φ grid and back was developed;
  Adaptation of CONV2D in a part of coordination with the oxidation 1-D module of the grid data was carried out.
A simulation of joint work of the melt-steel oxidation 1-D module with the corium melt 2-D thermo-hydraulic code was carried out:
  Data from CONV2D were manually transferred to the input desk of the 1-D module and the adequate outcome was received.
The new code is ready for testing and verification against available experimental data and benchmark tests.
Notes: f;jhg;\jd
10

## Slide 11: Perspectives: Application of New Code to Analysis of SA in Fast Reactors
Effect of rapid eutectic penetration in vessel steel interacting with hot ceramic material (fuel or crust) is one of the key topics for safety analysis of Fast Reactors : “The normal melting point of the steel is around 1700 K, but chemical interactions between fuel and the steel components are likely to lower the effective melting temperature of the steel. The rapid eutectic penetration temperature is approximately 1400 K. Melt-through of the reactor vessel might occur if direct contact with fuel was established and the vessel cooling was insufficient to maintain the local wall temperature below the effective melting temperature” [SA research Review paper for Fast Breeder Reactors, Report ANL-2010]
A similar effect is also important for the meltdown of small bundles in slow-power transients or transients resulting from cooling losses, studied in the French tests SCARABEE, where rapid liquefaction of steel wrapper by U-Zr-O corium was observed
METCOR tests provide some important microstructure observations that allow qualitative understanding of the accelerated steel corrosion (via extrusion of eutectic melt) observed also in the integral tests, and quantitative interpretation of the SCARABEE tests observations using the new corrosion model developed in the THOMAS Project

## Slide 12: SCARABEE tests

## Slide 13: Physical mechanisms of enhanced SS corrosion at high temperatures
“Flowering” mechanism:
  formation of FeO/crust eutectic melt and its extrusion (or “drainage”) through the crust
Low temperatures
High temperatures
Melt
Crust
FeO
Initial position of Fe boundary
Compressive stresses
Tensile stresses
Cracks and tears
Melt
Crust
FeO
Eutectics
Melt
SS
SS

## Slide 14: Application of 1D corrosion model to conditions of SCARABEE tests (preliminary results)
Calculated corrosion kinetics at different heat and oxygen fluxes
Oxygen flux 10-2 kg/m2s1
Oxygen flux 10-1 kg/m2s1

## Slide 15: Comments to the calculation results (stand-alone 1D corrosion model)
Under conditions of high heat flux >5106 W/m2 , temperature at the steel surface is above the steel melting point ( 1673 K)  direct melting of a steel layer and of pre-existing oxide (FeO) layer (Tmelt  1644 K) during a short initial period of 1-10 s
Further growth of corrosion layer is controlled by the oxygen flux, via the flowering mechanism
In these calculations heat and oxygen fluxes were independent input values (evaluated from the experimental data); in reality they are strongly inter-related via the thickness of the convection boundary layer and can be generally calculated using the thermal-hydraulic code with the implemented corrosion model (further improved and modified for the extreme conditions of SCARABEE tests)
This development might be a topic for a future Project, as well as extension of CONV2D with the implemented melt oxidation-steel corrosion model to more general consideration of Fe-U-Zr-O corium (with melt stratification effect) and elaboration of 3D-version of the new code