## Slide 1
ESTIMATED EXPERIMENTAL RESEARCHES TO CHARACTERIZE HIDDEN NUCLEARLY HAZARDOUS
CLUSTERS OF FUEL CONTAINING MATERIALS
IN DESTROYED ChNPP UNIT 4
Institute for safety problems of NPPs National Academy of sciences of Ukraine Chernobyl, 2008
UNAS Cor. Memb. TSD Klyuchnykov O.O., TSC – Vysotskiy E.D. PMSC- Shostak V.B.
Notes: 1

## Slide 2
Reactor basis (RB)
South-east quadrant of under reactor room. Lava fuel containing materials (LFCM) formation and outcome place
Reactor foundation plate – 2 meters of monolith concrete
Fig. 1. Reactor vault and under reactor room 305/2 after accident (reconstruction)
Room 304/3

## Slide 3
Drill boreholes
Melting-through areas
Fig. 2. Boreholes in foundation plate
Black ceramics
Drilling boreholes in direction to premises 305/2 were carried out in 1987-1990 with the aim to identify LTCN layout boundaries.
Drilling process was stopped, when the activity of withdrawn cores testified the fact, that drilling tool entered a LTCM cluster with high fuel content.
Considering the above, one should assume that bottom holes of such boreholes, which were not drilled to the end (З.9.Ф, З.9.Ж, З.9К, З.9.Е, Ю.9.Б, Ю.9.В), reached the boundaries of LTCM clusters with high fuel content hidden under the concrete.
З.9.Л

## Slide 4
Fig. 3. Temperature measurements
Temperature fields in FP room 305/2 (October, 1988)
Temperature fields indicated the presence of heat emanation sources in separate parts of subreactor plate.
Measurements of heat flows enabled making approximate evaluation of fuel amount within the area of clusters (around 50 tons uranium).
Currently, temperature within the area of cluster located in south-east part of premises 305/ 2 exceeds the temperature on subreactor plate peripheria at more than 20 °С (Fig. 4). Outflow of warm water is periodically observed within the cluster area

## Slide 5
Fig. 4. Dynamics of temperature changes on melting area periphery and foundation plate

## Slide 6
UO2 (maximum) = 30 %
Fig. 5. Model &
neutron-flux density distribution

## Slide 7
Channel count speed, imp/sec.
c) Self-dumping of incident occurred after 36 hours as result of probable over-wetting of multiplying medium of clusters.
Currently, clusters are permanently located in water, whose level does not drop below building mark + 9.10 m.
а) Neutron sensors located in neighboring premises 304/3, fixed consequent increase in flux density of neutron leak (via 1-m concrete wall) from premises 305/2 in more than 60 times (1-4*10-3 β)
b) Filling of neutron absorber -gadolinium led to sensors blocking
Fig. 6. Neutron incident in room 305/2, June, 1990. Neutron detector reading in room 304/3
- control points

## Slide 8
Fig. 7. Temperature in foundation plate, 1988-1991
а) In early 1990, clusters temperature dropped below 100 °С
b) Water coming via roofing cracks into «Shelter» object during March – April 1990 and intensive precipitation in June resulted in impregnation of LFCM clusters with water.
A version of incident reasons was water penetration within clusters area.
Period of intensive precipitation in 1990
Release of energy
(relative units)

## Slide 9
Fig. 8. FCM organization process and cluster structure
Southern melted-through area surrounded by “charge”, which is formed in result of explosion and destruction of active zone (AZ). “Charge” around concrete area fully melted and burned out. Fuel is sinked in melted-through area.
LFCM cluster, covered by “fresh” concrete layer
Graphite, active zone fragments, metal, filling up materials
“fresh” concrete, 0,5 m
Concrete

## Slide 10
Fig. 9. Dependence of binary system (UO2+SiO2)Kef with total concrete reflector under concentration of UO2 – 40%, U235 – 1,2%
Multiplying system is modelled in geometry written in size of southern meling area. Binary system has homogenous structure with porosity from 40 to 60%. U235 concentration to 1,0-1,2% corresponds to burnup of 11-13 MW*day/kg (U). Model height is restricted by water level in melting area. Calculations was made in MCNP-4 software complex.
Today, foundation plate LFCM are located in water in subcritical state.
а) In 1988, temperature in LFCM clusters was above 200°C.
water volume, %
b) At the beginning of the 1990, temperature in clusters dropped below 100°C and LFCM appears in water. In June, 29 1990 was peak of neutron incident.

## Slide 11
Fig. 10. Multiplying system reactivity within optimal damping area
(UO2 – 40%, U235 – 1,2%)
Minimal geometry of cylinder

## Slide 12
Fig. 11. System reactivity in optimal damping area
(UO2 - 50-55%; U235 - 1%)
Burning increase ubder tge same system volume leads to offset of higher fuel concentration, as well as to increase in needed volumes of moderator.

## Slide 13
Fig. 12. Northern melted-through area
Concrete pedestal
“grotto”
Melted-through area
“fresh” concrete